03848WEP-HFX/03849CEH-HFX Two Component 2.5 VOC HAP's Free/Exempt White Epoxzen Primer per MIL-DTL-53022D, Type III

| # PRODUCT DESCRIPTION EPOXZEN is the trade name for Hentzen's Epoxy Coatings. This two-component primer is formulated to meet the performance requirements of MIL-DTL-53022D, Type III. # HANDLING & STORAGE The containers should be stored away from direct sunlight and heat. Freezing is not harmful if reheated gently to room temperature prior to use. # PHYSICAL CHARACTERISTICS 03848WEP-HFX HAP's Free White Epoxzen - Component A: Weight per Gallon: 12.68 lbs. ± .25 Weight Solids: 71.15% ± 2.0% Volume Solids: 50.31% ± 2.0% Viscosity: 65 – 70 KU's Flash Point: 9oF 03849CEH-HFX-NO Epoxy Hardener - Component B: Weight per Gallon: 7.61 lbs.± .25 Weight Solids – Theoretical: 39.47% ± 2.0% Volume Solids: 35.28% ± 2.0% Viscosity: 20-25" #2 Zahn Flash Point: 9oF Admixed Characteristics: Catalyzation Ratio: 4:1 by volume Weight per Gallon: 11.66 lbs. ± .30 Weight Solids: 67.02% ± 2.0% Volume Solids: 47.25% ± 2.0% VOC: 2.46 theo. Viscosity: 14-21" #3 Zahn Theoretical Coverage - sq. ft./gl. @ 1.0 mil dry film thickness: 758.8 Useable Pot Life: Approximately 4 hours to 1½ times initial viscosity. To extend the pot life, regulations permitting, some additional thinner may be required to reduce the viscosity. A fresh mixture of Component A and B could also be added to lower the pot viscosity | Gloss @ 60o Meter: 10 - 30 @ 2.0 mil draw down Cure Schedule - Air Dry @ 77oF & 50% Relative Humidity: Set to Touch: 30 minutes Dry Hard: 4 hours Dry Through: 6 hours Recoat: 1 – 2 hours Full Resistance Properties: 7 days Force Cure Recommendation: 15 minutes @ 180oF # ENVIRONMENTAL REPORT Volatile Content (Wt.%): 32.98 Organic Volatile Content (Wt.%): 15.57 Density of Organic Volatile (Wt./Gl.): 6.91 Density of Solid Content (Wt./Gl.): 16.54 Exempt Solvent Content (Wt.%): 17.41 Exempt Solvent Content (Vol.%): 26.11 VOC Minus Water: 2.50 maximum # DIRECTIONS FOR USE Component A should be thoroughly agitated prior to blending. After agitating Component A, mix 4 volumes of Component A to 1 volume of Component B and mix the two Components well. Allow the admixed product 30 minutes to induct prior to spraying. No further reduction is necessary. Mix only what you will use in 4 hours. After that time, the product will have gained viscosity and will eventually gel. # PRECAUTIONS & SAFETY - Do not apply at temperatures below 50oF. - Read all container labels. - Read Material Safety Data Sheet. - Keep away from open flame and sparks. # CLEAN-UP Clean equipment immediately after use with 00212SST-1 Solvent Blend or equivalent. May 17, 2010 |
| --- | --- |