| 04488WEP-4/04489CEH-4 Two Component Off-White High Solids Epoxzen Primer per MIL-P-53022B, Type II |  |  |
| --- | --- | --- |
| ### PRODUCT DESCRIPTION EPOXZEN is the trade name for Hentzen's Epoxy Coatings. This two component primer meets the requirements of MIL-P-53022B. ### HANDLING & STORAGE The containers should be stored away from direct sunlight and heat. Freezing is not harmful if reheated gently to room temperature prior to use. ### PHYSICAL CHARACTERISTICS 04488WEP-4 Off-White Epoxzen - Component A: Weight per Gallon: 12.85 lbs.  .35 Weight Solids: 75.26  1.00% Volume Solids: 54.17  1.00% Viscosity: 65 - 75 KU's 04489CEH-4 Epoxy Hardener - Component B: Weight per Gallon: 8.02 lbs.  .25 Weight Solids: 39.29  1.00% Volume Solids: 33.86  1.00% Viscosity: 40 - 50" @ #3 Zahn Admixed Characteristics: Catalyzation Ratio: 4:1 by volume Weight per Gallon: 11.88 lbs.  .35 Weight Solids: 70.41  1.00% Volume Solids: 50.11  1.00% VOC: 3.41 maximum Viscosity: 22 - 32" @ #3 Zahn Theoretical Coverage - sq. ft./gl. @ 1.0 mil dry film thickness: 803.8 Useable Pot Life: Approximately 4 - 8 hours to 1½ times initial viscosity. To extend the pot life, regulations permitting, some additional thinner may be required to reduce the viscosity. A fresh mixture of Component A and B could also be added to lower the pot viscosity. | Gloss @ 60o Meter: 10 - 30 @ 1.0 mil DFT Cure Schedule - Air Dry @ 77oF & 50% Relative Humidity: Set to Touch: 10 - 20 minutes Dry Hard: 1 - 1½ hours Dry Through: 24 hours Recoat: 2 - 24 hours Full Resistance Properties: 7 days Force Cure Recommendation: 20 - 30 minutes @ 180oF ### ENVIRONMENTAL REPORT Volatile Content (Wt.%): 29.58 Organic Volatile Content (Wt.%): 28.08 Density of Organic Volatile (Wt./Gl.): 6.88 Density of Solid Content (Wt./Gl.): 16.70 Exempt Solvent Content (Wt.%): 1.51 Exempt Solvent Content (Vol.%): 2.31 VOC Minus Water: 3.41 maximum ### DIRECTIONS FOR USE Component A should be thoroughly agitated prior to blending. After agitating Component A, mix 4 volumes of Component A to 1 volume of Component B and mix the two Components well. Allow the admixed product 30 minutes to induct prior to spraying. No further reduction is necessary. Mix only what you will use in 4 hours. After that time, the product will have gained viscosity and will eventually gel. ### PRECAUTIONS & SAFETY - Do not apply at temperatures below 50oF. - Read all container labels. - Read Material Safety Data Sheet. - Keep away from open flame and sparks. ### CLEAN-UP Clean equipment immediately after use with 00212SST-1 Solvent Blend or equivalent. January 20, 2004 |  |