16708TEP/16709CEH MIL-PRF-23377J Type I Class N

| # PRODUCT DESCRIPTION EPOXZEN is the trade name for Hentzen's Epoxy Coatings. This chromate-free primer is qualified to MIL-PRF-23377J Type I, Class N Specification. ## HANDLING & STORAGE The containers should be stored indoors at 60-90oF. # PHYSICAL CHARACTERISTICS 16708TEP Beige Epoxzen - Component A: Weight per Gallon: 12.7 lbs.  0.2 Weight Solids: 79.6%  1.0 Volume Solids: 62.1%  1.0 16709CEH Epoxy Hardener - Component B: Weight per Gallon: 7.5 lbs.  .25 Weight Solids: 49.6%  1.0 Volume Solids: 43.9%  1.0 Admixed Characteristics: Catalyzation Ratio: 3:1 by volume Weight per Gallon: 11.4 lbs.  0.2 Weight Solids: 74.7%  1.0 Volume Solids: 56.5%  1.0 VOC: 340 g/l Viscosity: 20 - 25" @ #4 Ford Theoretical Coverage - ft2/gl. @ 1.0 mil dry film thickness: 923 Pot Life: 4 hours Induction Time: None Gloss @ 60° @ 0.6 - 0.9 mil DFT: 10 max. | Cure Schedule@ 77oF & 50% Relative Humidity: Tack Free: 90 min. Time to Topcoat: 3 hours min. Dry Hard: 6 hours Full Resistance Properties: 7 - 10 days # ENVIRONMENTAL REPORT Volatile Content (Wt.%): 25.3 Organic Volatile Content (Wt.%): 25.3 Water Content (Wt.%): 0.00 Water Content (Vol.%): 0.00 VOC Minus Water: 340 g/l # DIRECTIONS FOR USE Components A should be thoroughly agitated prior to blending. After agitating Component A, mix 3 volume of Component A to 1 volume of Component B and mix the two Components well. No induction time is needed. Use up the admixed primer within 4 hours under ambient temperature to ensure optimum properties. # PRECAUTIONS & SAFETY - Do not apply at temperatures below 50oF. - Read all container labels. - Read Material Safety Data Sheet. - Keep away from open flame and sparks. # CLEAN-UP Clean equipment immediately after use with aromatics or ketones. March 1, 2006 |
| --- | --- |