16959AEF-LVOC/16062CEH-LVOC Two Component Gray Gloss Epoxzen, Fed. Std. Color #16081 Per MIL-PRF-22750F

| PRODUCT DESCRIPTION EPOXZEN is the trade name for Hentzen's epoxy coating. This product is a two component catalyzed system that will meet or exceed the performance of MIL-PRF-22750F. HANDLING & STORAGE The containers should be stored away from direct sunlight and heat. Freezing is not harmful if reheated gently to room temperature prior to use. PHYSICAL CHARACTERISTICS 16959AEF-LVOC Gray Gloss Epoxzen - Component A: Weight per Gallon: 10.90 lbs. ± .35 Weight Solids: 59.47% ± 1.0 Volume Solids: 45.74% ± 1.0 Viscosity: 47 - 53 KU's 16062CEH-LVOC Clear Epoxy Hardener - Component B: Weight per Gallon: 9.24 lbs. ± .25 Weight Solids: 45.00% ± 1.0 Volume Solids: 46.70% ± 1.0 Viscosity: 35 - 45" #4 Ford Admixed Characteristics: Catalyzation Ratio: 3:1 by volume Weight per Gallon: 10.49 lbs. ± .35 Weight Solids: 56.29% ± 1.0 Volume Solids: 45.98% ± 1.0 VOC: 1.80 maximum Viscosity: 16 - 22" #4 Ford Theoretical Coverage - sq. ft./gl. @ 1.0 mil dry film thickness: 737.5 Useable Pot Life: Less than 70" #4 Ford Cup in 4 hours - not gelled in 8 hours Gloss @ 60o Meter: 90+ @ 2.0 mils | Cure Schedule - Air Dry @ 77oF & 50% Relative Humidity: Dry to Touch: <4 hours Dry Hard: <8 hours Recoat Up To: 72 hours Full Resistance Properties: 7 days ENVIRONMENTAL REPORT Volatile Content (Wt.%): 43.71 Organic Volatile Content (Wt.%): 10.30 Exempt Solvent Content (Wt.%): 33.41 Exempt Solvent Content (Vol.%): 38.94 VOC Minus Water: 1.80 max. DIRECTIONS FOR USE Component A should be thoroughly agitated prior to blending. After agitating Component A, mix 3 volumes of Component A to 1 volume of Component B and mix the two Components well. Allow the admixed product 30 minutes to induct prior to spraying. No further reduction is necessary. Mix only what you will use in 4 hours. Viscosity increase will occur when admixed. PRECAUTIONS & SAFETY - Do not apply at temperatures below 50oF. - Read all container labels. - Read Material Safety Data Sheet. CLEAN-UP Clean equipment immediately after use with 00212SST-1 Solvent Blend or equivalent. March 12, 2004 |
| --- | --- |