17176KEP/16709CEH MIL-PRF-23377J Type II, Class N

| # PRODUCT DESCRIPTION EPOXZEN is the trade name for Hentzen's Epoxy Coatings. This chromate-free primer is qualified to MIL-PRF-23377J Type II, Class N Specification. ## HANDLING & STORAGE The containers should be stored indoors at 60 - 90°F. # PHYSICAL CHARACTERISTICS 17176KEP Dark Green Epoxzen - Component A: Weight per Gallon: 12.6 lbs. ± .2 Weight Solids: 80.0% ± 1.0 Volume Solids: 62.9% ± 1.0 16709CEH Epoxy Hardener - Component B: Weight per Gallon: 7.5 lbs. ± .2 Weight Solids: 49.6% ± 1.0 Volume Solids: 43.9% ± 1.0 Admixed Characteristics: Catalyzation Ratio: 3:1 by volume Weight per Gallon: 11.4 lbs. ± .2 Weight Solids: 75.0% ± 1.0 Volume Solids: 58.2% ± 1.0 VOC: 340 g/l Viscosity: 20 - 25" @ #4 Ford Theoretical Coverage - sq. ft./gl. @ 1.0 mil dry film thickness: 934 Pot Life: 4 hours @ 77°F Induction Time: None Gloss@ 60° @ 0.6 - 0.9 mil DFT: 10 max. | Cure Schedule@ 77oF & 50% Relative Humidity: Tack Free: 90 minutes Time to Topcoat: 3 hours min. Dry Hard: 6 hours Full Resistance Properties: 7 - 10 days # ENVIRONMENTAL REPORT Volatile Content (Wt.%): 25.0 Organic Volatile Content (Wt.%): 25.0 Water Content (Wt.%): 0.00 Water Content (Vol.%): 0.00 VOC Minus Water: 340 g/l # DIRECTIONS FOR USE Components A should be thoroughly agitated prior to blending. After agitating component A, mix 3 volume of Component A to 1 volume of Component B and mix the two Components well. No induction time is needed. Use up the admixed primer within 4 h under ambient temperature to ensure optimum properties. # PRECAUTIONS & SAFETY - Do not apply at temperatures below 50oF. - Read all container labels. - Read Material Safety Data Sheet. - Keep away from open flame and sparks. # CLEAN-UP Clean equipment immediately after use with aromatics or ketones. October 17, 2006 |
| --- | --- |