53012YEP/16709CEH MIL-PRF-23377J Type I Class C1.

| # PRODUCT DESCRIPTION This is a Barium Chromate Primer that meets the requirements of Mil-PRF-23377J Type I Class C1. ## HANDLING & STORAGE The containers should be stored indoors at 60-90oF. # PHYSICAL CHARACTERISTICS 53012YEP- Component A: Weight per Gallon: 12.3 lbs.  0.2 Weight Solids: 77.1%  1.5 Volume Solids: 59.0%  1.5 16709CEH - Component B: Weight per Gallon: 7.5 lbs.  .25 Weight Solids: 49.6%  1.0 Volume Solids: 43.9%  1.0 Admixed Characteristics: Catalyzation Ratio: 3:1 by volume Weight per Gallon: 11.1 lbs.  0.2 Weight Solids: 72.5%  1.5 Volume Solids: 55.3%  1.5 VOC: 340 g/l Viscosity: 20-25" Zahn 2 Theoretical Coverage - ft2/gl. @ 1.0 mil dry film thickness: 887 Pot Life: 4 hours Induction Time: None Gloss @ 60° @ 0.6 - 0.9 mil DFT: 20 max. | Cure Schedule@ 77oF & 50% Relative Humidity: Tack Free: 90 min. Time to Topcoat: 3 hours min. Dry Hard: 6 hours Full Resistance Properties: 7 - 10 days # ENVIRONMENTAL REPORT Volatile Content (Wt.%): 27.5 Organic Volatile Content (Wt.%): 24.8 Exempt Content (Wt.%): 2.7 Exempt Content (Vol.%): 4.2 VOC Minus Exempt: g/l 340 # DIRECTIONS FOR USE Components A should be thoroughly agitated prior to blending. After agitating Component A, mix 3 volume of Component A to 1 volume of Component B and mix the two Components well. No induction time is needed. Use up the admixed primer within 4 hours under ambient temperature to ensure optimum properties. # PRECAUTIONS & SAFETY - Do not apply at temperatures below 50oF. - Read all container labels. - Read Material Safety Data Sheet. - Keep away from open flame and sparks. # CLEAN-UP Clean equipment immediately after use with aromatics or ketones. October 3, 2007 |
| --- | --- |