### T E C H N I C A L D A T A S H E E T

# MIL-PRF-85285E

# TYPE II , CLASS H

# URA-ZEN HIGH SOLIDS TOPCOAT

## PRODUCT DESCRIPTION

URAZEN is a two component, high solids polyurethane topcoat that is qualified to MIL-PRF-85285E, Type II, Class H for ground support applications.  It exhibits excellent chemical resistance, outstanding toughness, flexibility, abrasion resistance, and excellent outside durability.  This product is available in full gloss, semi-gloss, and flat gloss ranges.

## TECHNICAL DATA

- Mixing Ratio by Volume: 3:1 Part A with Part B, 06480CMU

- Admixed Viscosity:  <30 sec #4 Ford.

Viscosities will vary with each color and gloss range.

- Recommended dry film thickness: 1.7-2.3 mils

- Gloss 60˚:

Full gloss:  90+

Semi-gloss: 15-45

Flat: <5

- Flash Point: 9˚ F

- VOC:  2.8 lbs./gal.  or 340 grams/liter

- Cure Rate – Air Dry @77˚ and 50% relative humidity:

Set: 	   <2 hours

Dry Hard:  <8 hours

Full Cure:  2 weeks

This product may be force cured if necessary.  The recommended schedule is 30-60 minute flash, then 30-60 minutes at 140-160˚F.  Semi-gloss and flat coatings may increase slightly in gloss with force curing.

## DIRECTIONS FOR USE

Component A should be thoroughly agitated prior to blending.  After agitating, mix 3 volumes of Component A to 1 volume of Component B and mix well.  Mix only what you will use in 4 hours.  After that time, the product will start to rise in viscosity and eventually gel

## SURFACE PREPARATION

Substrate must be free of dirt, rust, grease and other contaminants to ensure optimal performance of the coating.   Prime surface with one coat of epoxy primer at 0.6 to 0.9 mil dry film thickness and air dry per manufacturers recomendations prior to spraying topcoat.   See page 2 for recommended primers.

REV. Jan 2008

### T E C H N I C A L D A T A S H E E T Page 2

# MIL-PRF-85285E

# TYPE II , CLASS H

URA-ZEN HIGH SOLIDS TOPCOAT

#### APPLICATION

Apply topcoat at temperatures between 60-90˚F and 20-80% relative humidity.  Spray one or two coats uniform wet coats to achieve a dry film thickness of 1.7-2.3 mils topcoat.

Product can be reduced if necessary with ketones such as Methyl Amyl Ketone, Hentzen part number 07409SSK.  Typically, reduction should not exceed 25% by volume, 4 parts mixed paint to 1 part reducer, to yield a VOC under 3.50. An exempt solvent may also be used as a reducer. The recommended solvent is Methyl Acetate, Hentzen part number 01574SSE.

## CLEAN-UP

Clean equipment immediately after use with MEK, 07409SSK, or equivalent solvent reducer.

## HANDLING & STORAGE

The containers should be stored away from direct sunlight and heat.  Freezing is not harmful if reheated gently to room temperature prior to use. For best results, maintain storage temperatures between 50 and 100˚F.

## PRECAUTIONS & SAFETY

- Flammable liquid.

- Use only with adequate ventilation.

- Keep away from heat, sparks and flame.

- Harmful if inhaled or ingested, may cause nose, throat, and respiratory tract irritation

- Skin and eye irritant.

- Read all container labels and Material Safety Data Sheet prior to use.

## RECOMMENDED PRIMERS AND REDUCERS

| RECOMMENDED PRIMERS | DESCRIPTION | SPECIFICATION |
| --- | --- | --- |
| 05510WEP-X/05511CEH-X | Off White Epoxy Primer | MIL-P-53022B, TYPE I |
| 04488WEP-4/04489CEH-4 | Off White Epoxy Primer | MIL-P-53022B, TYPE II |
| 03848WEP-HFX/03849CEH-HFX | Off White Epoxy Primer | MIL-P-53022B, TYPE II |
| 16708TEP/16709CEH | Chromate-Free Epoxy Primer | MIL-PRF-23377J, TY I, CLS N |
| AD9318-FD/AD2298-FD | Fast Dry Yellow Epoxy Primer | MIL-PRF-23377J, TY I, CLS C2 |
| RECOMMENDED REDUCERS |  |  |
| 00053SST-1 | Epoxy & Urethane Thinner | MIL-T-81772B, TYPE I |
| 07409SSK | Methyl Amyl Ketone Reducer |  |
| 01574SSE | Methyl Acetate Reducer |  |

### T E C H N I C A L D A T A S H E E T Page 3

# MIL-PRF-85285E

# TYPE II , CLASS H

URA-ZEN HIGH SOLIDS TOPCOAT

## PRODUCT PART NUMBERS

| FED-STD-595 COLOR | HCI PART NUMBER | DESCRIPTION |
| --- | --- | --- |
| Component A |  |  |
| 11136 | 32211RPX-T2 | Red Gloss Ura-Zen |
| 12197 | 32234NPX-T2 | Orange Gloss Ura-Zen |
| 13538 | 32202YPX-T2 | Yellow Gloss Ura-Zen |
| 15044 | 32237BPX-T2 | Blue Gloss Ura-Zen |
| 15180 | 32209BPX-T2 | Blue Gloss Ura-Zen |
| 16081 | 32213APX-T2 | Gray Gloss Ura-Zen |
| 16440 | 32212APX-T2 | Gray Gloss Ura-Zen |
| 17038 | 32204KPX-T2 | Black Gloss Ura-Zen |
| 17875 | 32236WPX-T2 | White Gloss Ura-Zen |
| 17925 | 32201WPX-T2 | White Gloss Ura-Zen |
| 24052 | 32206GPX-T2 | Green Semi-Gloss Ura-Zen |
| 24300 | 32207GPX-T2 | Green Semi-Gloss Ura-Zen |
| 26231 | 32274APX-T2 | Gray Semi-Gloss Ura-Zen |
| 26307 | 32215APX-T2 | Gray Semi-Gloss Ura-Zen |
| 27875 | 32218WPX-T2 | White Semi-Gloss Ura-Zen |
| 34095 | 32225GPX-T2 | Green Flat Ura-Zen |
| 34097 | 32233GPX-T2 | Green Flat Ura-Zen |
| 35237 | 32238BPX-T2 | Blue Flat Ura-Zen |
| 36231 | 32239APX-T2 | Gray Flat Ura-Zen |
| 36320 | 32240APX-T2 | Gray Flat Ura-Zen |
| 36375 | 32221APX-T2 | Gray Flat Ura-Zen |
| 36440 | 32249APX-T2 | Gray Flat Ura-Zen |
| 36495 | 32245APX-T2 | Gray Flat Ura-Zen |
| 37038 | 32205KPX-T2 | Black Flat Ura-Zen |
| Component B |  |  |
| n/a | 06480CMU | High Solids Ura-Zen Catalyst, Part B |
| Other FED-STD-595 colors as well as custom colors available upon request. |  |  |

REV. Jan 2008